Liquid Scintillator Research for the 280m Near Detector

to be used in the T2K Neutrino Oscillation Experiment

Patrick Bonnick, Chemical Physics, Semester 4

TRIUMF

December 21, 2004

84 Queensdale Crescent

Guelph, ON, N1H 6W3

(519) 829-1748

January 5, 2005

Dr. Jimmy Law

224 MacNaughton Building

University of Guelph

Guelph, ON, N1G 2W1

(519) 824-4120 Ext. 53021

Dear Dr. Law,

I recently had the pleasure of spending my second work term at TRIUMF in British Columbia.  During my time there, I researched the liquid scintillator that is going to be used in the 280m Near Detector as part of the Tokai to Kamioka (T2K) Neutrino Oscillation Experiment.  My primary responsibility was to produce a clear liquid scintillator that had a high photon emittance and a high water concentration to be used as the detection medium in the Near Detector.  Additionally, I performed tests on materials that were going to be incorporated into the Near Detector design to determine whether or not they would perform as required.  I worked directly under Dr. Stanley Yen, and our Neutrino group leader was Dr. Akira Konaka.

The conclusion of the solar neutrino detection experiments conducted at SNO in 2001 confirmed that neutrinos oscillate between e, ,  and mixtures of all three while on route to the Earth from the Sun.  Since then, attempts to better understand neutrino oscillations have sprung up and many theories are currently under scrutiny.  The T2K experiment hopes to narrow down the field of possible explanations by testing the rate that  turn into e over a distance of 295km.  To detect a change from one neutrino type to another, the number of neutrinos of each type must be known at the source (280m Near Detector) and at the end of the baseline.  The Near Detector will be placed 280m beyond the neutrino source (JPARC) and the Far Detector, Super Kamiokande, will detect the neutrinos when they reach Kamioka, Japan, which is 295km from Tokai, Japan.  The Near Detector is currently planning to use long, thin, square tubes to hold a liquid scintillator that will detect the neutrinos.  This liquid scintillator must be clear, have a high photon emittance and a high water concentration to minimize the difference between the two detection mediums (i.e. the scintillator in the Near Detector and water in the Far Detector).  This report deals with the research performed on the liquid scintillator.

My report is written in a journal article style and is aimed at an audience with my level of education; although, some previous knowledge of neutrinos would be an asset.  The report was edited by my supervisor, Dr. Yen, and by Dr. Sabesh Kanagalingam, my previous supervisor at BTI in Chalk River.

Sincerely,

Patrick Bonnick

Liquid Scintillator Research for the 280m Near Detector

to be used in the T2K Neutrino Oscillation Experiment

Name:	Patrick Bonnick

Student ID:	0181884

Last Semester Completed:	4

Department:	Physics

College:	CPES

Date:	December 21, 2004

Table of Contents

- Introduction	2

- Background Knowledge

  - The History	2

  - The Tokai to Kamioka (T2K) Project	3

    - Overview	3

    - Current Near Detector Proposal	4

  - The Physics	5

    - Of Muon Neutrino Creation	5

    - Of Neutrino Detection in Liquid Scintillators	6

    - Of Wavelength Shifting Fibers (WSF)	6

- Progress on the Near Detector

  - Liquid Scintillator Development	7

  - Gel Scintillator Development	9

  - Material Resistance Tests	10

    - Fiber Degradation	10

    - Plastic Survival Challenge	13

  - Biological Inhibiter Issues	15

  - Beam Tests	15

    - Liquid Cocktails	15

    - PPO/POPOP	18

  - Prototype Tests	19

    - Prototype 1	19

    - Carbopol EZ-3 Gels and Leaks	21

    - Coroplast	22

    - Prototypes 2 and 3	24

- Discussion and Conclusions

  - Regarding Beam Tests	25

    - Light Output	25

    - PPO/POPOP	25

    - Natural Gels	26

  - Regarding Carbopol Gels	27

  - Regarding Material Resistance Tests	28

  - Regarding Biological Inhibiters	29

  - Regarding Prototypes	30

- Where to Next?	30

Acknowledgements	32

References	32

Bibliography	32

Appendix:  Recipes

Standard 20mL Liquid Cocktail	33

Standard 20mL Carbopol Gel	33

50mL of ~2wt% (~0.5M) NaOH	34

0.1g Carbopol per 5mL Water Stock Solution	34

List of Tables and Figures

Table 1:  The phases of various 20mL cocktails at 25ºC.  The presented ranges represent the vol% of QSA present in the cocktails made with the listed vol% of water.  Triton comprises the rest of the vol% in all cases.	8

Table 2:  Clear, 20mL cocktails at 23ºC	9

Table 3:  Cloud point of various cocktails	9

Table 4:  Clear, 20mL Carbopol Gels at 25C	10

Table 5:  Quicksafe A resistance of various materials.  These observations were made on December 8, 2004	14

Table 6:  Declining water level in Coroplast detection cells sealed with RTV Sealant	23

Table 7:  Light yield of Prototypes 2 and 3 at a distance of 136mm from the PMT “Patrick”, at a voltage of –2150V and an attenuator setting of 1.0.  The prototypes were filled with a 50/47.5/2.5 cocktail	25

Figure 1:  Proposed organization of detection cells in the Near Detector.  Each sheet of cells will be a single extruded piece of diffusely reflective material that can withstand chemical attack by the scintillation cocktail.  The cells are orientated in an alternating horizontal and vertical pattern to provide a 3D readout of the charged particles traveling through the Near Detector.  Wavelength shifting fibres will run the length of the cells and transmit events from the cells to photomultiplier tubes	4

Figure 2:  Diisopropylnaphthalene is the primary scintillator in Quicksafe A	8

Figure 3:  Wavelength shifting fibers with sections of core dissolved.  The bright material in the fiber is the intact polystyrene core.  The left photo is a notch, while the right photo is a fiber end	11

Figure 4:  Deterioration of the wavelength shifting fiber’s polystyrene core, in various 55% Quicksafe A cocktails.  These cocktails were incubated at 50ºC and separated over time.  “21/55/24” refers to a cocktail made of 21% water, 55% QSA and 24% Triton.  The distances refer to the length of hollowed out cladding surrounding the notch	12

Figure 5:  Deterioration of the wavelength shifting fiber’s polystyrene core in various 55% Quicksafe A cocktails.  These cocktails were incubated at 50ºC and separated over time.  “21/55/24” refers to a cocktail made of 21% water, 55% QSA and 24% Triton.  The distances refer to the length of hollowed out cladding measured from the fiber end	12

Figure 6:  Fibre degradation in a liquid cocktail and a Carbopol gel cocktail.  Both cocktails are 72/19/9 and have 3 WSFs.  The ‘Distance’ is the length of core that the cocktail has dissolved, extending from the exposed end of the fibre.  The error is ±0.2mm	13

Figure 7:  Vial testing apparatus.  The PMT is in the top left corner	16

Figure 8:  Number of photoelectrons emitted by cocktails with various concentrations of Quicksafe A.  The error is ±3 photoelectrons	17

Figure 9:  Light output of scintillator cocktails made with Triton X-100/PPO/POPOP.  The concentration of PPO/POPOP is 0g, 1g and 2g per 50mL of Triton X-100	18

Figure 10:  Prototype 1 after assembly and an un-assembled custom tube head.  The custom tube head threads on to a PMT once assembled	20

Figure 11:  Light yield collected by 3 Wavelength Shifting fibers, immersed in a 70/27.5/2.5 cocktail, as the distance from the snout of the PMT to the beam's path is increased	21

Figure 12:  End view of a piece of trimmed Coroplast.  The walls between cells are 0.5mm thick, the exterior walls are 0.7mm thick and each cell’s dimensions are 8.5mm × 8.5mm	22

Figure 13:  These two photos show how the set of 4 detection cells were insulated first with black electrical tape and then with aluminum foil to prevent evaporation	23

Figure 14:  Both ends of the 50cm long Prototype 2 and 3.  The left photo shows the unsealed second plug.  The right photo shows the Lucite Tube, vial cap and WSF	24