General Research and Prototyping for the 280m Near Detector

to be used in the T2K Neutrino Oscillation Experiment

Patrick Bonnick, Chemical Physics, Semester 5

TRIUMF

September 22, 2005

84 Queensdale Crescent

Guelph, ON, N1H 6W3

(519) 829-1748

September 22, 2005

Dr. Ernie McFarland

435D MacNaughton Building

University of Guelph

Guelph, ON, N1G 2W1

(519) 824-4120 Ext. 53653

Dear Dr. McFarland,

I recently had the pleasure of returning to TRIUMF, on UBC campus, for my third work term.  During my time there, I performed general research and produced several prototypes of a Fine Grained Detector (FGD) that is going to be used in the 280m Near Detector as part of the Tokai to Kamioka (T2K) Neutrino Oscillation Experiment.  The FGD will contain a water based liquid scintillator, which I perfected in my last coop work term.  My main task was to produce small scale prototypes of the FGD to test various aspects of the intended design.  I also performed several experiments on the liquid scintillator’s properties and on the durability of some materials intended for use in the FGD.  I worked directly under Dr. Stanley Yen, and our Neutrino group leader was Dr. Akira Konaka.

The conclusion of the solar neutrino detection experiments conducted at SNO in 2001 confirmed that neutrinos oscillate between e, ,  and mixtures of all three while on route to the Earth from the Sun.  Since then, attempts to better understand neutrino oscillations have sprung up and many theories are currently under scrutiny.  The T2K experiment hopes to narrow down the field of possible explanations by testing the rate that  turn into e over a distance of 295km.  To detect a change from one neutrino type to another, the number of neutrinos of each type must be known at the source (280m Near Detector) and at the end of the baseline.  The Near Detector will be placed 280m beyond the neutrino source (J-PARC) and the Far Detector, Super Kamiokande, will detect the neutrinos when they reach Kamioka, Japan, which is 295km from Tokai, Japan.  The Near Detector is currently planning to use long, thin, square tubes to hold a liquid scintillator that will detect the neutrinos.  Several aspects of this design must be controlled to produce the strongest possible light yield.  Such aspects include the reflectivity of the walls of the square tubes, the clarity of the liquid scintillator, the size of the wavelength shifting fiber that runs the length of the tube and the overall size of the FGD, which can control the loss of light due to attenuation.  This paper is concerned with the experiments performed to improve our understanding of how to optimize those aspects.

My report is written in a journal article style and is aimed at an audience with my level of education; although, some previous knowledge of neutrinos would be an asset.  The report was edited by my supervisor, Dr. Yen and my girlfriend.

Sincerely,

Patrick Bonnick

Prototyping and General Research for the 280m Near Detector

to be used in the T2K Neutrino Oscillation Experiment

Name:	Patrick Bonnick

Student ID:	0181884

Last Semester Completed:	5

Department:	Physics

College:	CPES

Date:	September 21, 2005

Table of Contents

Abstract	1

- Introduction	2

- The T2K Experiment

  - The Beam from J-PARC to Super Kamiokande	3

  - The 280m, off-axis Near Detector

    - Theoretical reasoning for the off-axis configuration2	4

    - The Near Detector’s water based scintillator containing Fine Grained Detector (FGD)	5

    - Currently favoured method of sealing the detection cells	7

  - Neutrino Oscillations

    - A simplified description of neutrino oscillations1	8

    - Research goals of the T2K experiment1,3	9

- Progress on the Fine Grained Detector

  - Cocktail Properties	11

    - Densities	12

    - Index of Refraction	12

    - PPO/POPOP	14

    - Cloud Point	15

    - Temperature Dependence of Light Yield	18

  - Construction Issues

    - Priming and painting the detection cells	19

    - Fiber size and configuration	22

    - Attenuation length	22

    - Cross talk tests	25

  - Material Durability Tests

    - Silicone oils	27

    - Leakage tests	28

    - Sealant durability tests	30

    - Long Term (LT) tests	33

- Conclusions

  - Regarding Cocktail Properties	34

  - Regarding Construction Issues	35

  - Regarding Material Durability Tests	36

- Recommendations	36

Acknowledgements	37

References	37

Bibliography	38

Appendix A:  Prototype construction instructions

Standard 52cm long prototype	38

Attenuation Length Prototypes	39

Cross Talk Prototypes	40

List of Tables and Figures

Table 1:  Calculation of the densities of Quicksafe A, Triton X-100 and a standard 70/25/5 cocktail.	12

Table 2:  Light yield of prototypes with a translucent Teflon tube sheathing the 1.0mm in diameter WSF.	13

Table 3:  Light yields of cocktails containing PPO/POPOP in various concentrations.	14

Table 4:  Cloud point of a standard 70/25/5 cocktail.	15

Table 5:  Cloud points of standard cocktails with varying amounts of Tergitol NP-13 or NP-15 surfactants added to them.	16

Table 6:  Light yields and water compositions of tested cocktails containing various amounts of NP-13 and/or NP-15.	17

Table 7:  Light yields of 52cm long, Matraplast prototypes utilizing different wavelength shifting fiber configurations.	22

Table 8:  Cross talk test results.	26

Table 9:  Summary of the silicone oil survival tests.	28

Table 10:  Declining water level in Coroplast detection cells sealed with RTV Sealant.	28

Table 11:  Light yields of the LT prototypes over the period of about four weeks.	33

Figure 1:  The momentum components of neutrinos emitted from a pion at rest, and from a pion that has been given a boost in the +x direction.	4

Figure 2:  Neutrino flux at increasing acute angles away from the axis of the decay pipe.	5

Figure 3:  The Near Detector.	6

Figure 4:  The currently favoured FGD design uses polypropylene panels of detection cells to hold the scintillation cocktail.	7

Figure 5:  Sketch of the design for sealing the ends of the detection cells.	7

Figure 6:  Analogy for explaining neutrino oscillations.	8

Figure 7:  Method of determining 23 and m232 by fitting a curve to the P data.	10

Figure 8:  Temperature dependence of 70/25/5 cocktail as tested in unpainted Matraplast prototypes, LT #9 and LT #10.	18

Figure 9:  Resultant quality of coats of paint, applied using different methods and materials.	21

Figure 10:  Attenuation length determination of the 1.0mm and 1.5mm WSFs in a 70/25/5 cocktail.	23

Figure 11:  Attenuation length graphs with sum-of-exponential fits.	25

Figure 12:  The crosstalk prototype consists of two detection cells side-by-side.	26

Figure 13:  Distance the water level in the sealed Coroplast cells dropped over time.	29

Figure 14:  The mass of RTV and Epoxy samples after prolonged exposure to 100% QSA at 50C.	31

Figure 15:  Mass of fluorinated silicone rubber samples during their incubation at either 21C or 29C.	32

Figure 16:  Standard 52cm long Matraplast prototype before the fiber ends were cut and polished.	39

Figure 17:  Cross talk prototype after production and light insulation.	40